## Slide 1
Investigation of Dislocation Density
of Directed Energy Deposited 316L Steel at Elevated Temperatures.
B.Tech Project Presentation
By
Jaya Vardhan
Supervisor: Dr. Eswara Prasad Korimilli
Discipline of Metallurgical Engineering and Materials Science
Indian Institute of Technology Indore

## Slide 2
Contents
Introduction
Literature Survey
Experimental Procedure
Results
Analysis

## Slide 3
316L Steel
Type 316L stainless steel is a molybdenum bearing austenitic. It is more resistant to general corrosion and pitting than conventional nickel chromium stainless steels such as 302-304.
L-grades can have a maximum carbon content of 0.03%. L-grades are resistant to sensitization in heat treatments. L-grade often have slightly lower strength than standard stainless steels.
Composition of 316L Steel:
https://www.lenntech.com/stainless-steel-316l.htm
Notes: Low Carbon – High Temperature Applications and Weldability.
C – Increases hardness and strength of Pure Iron.
Ni - Austenitic Stabilizer. (Non-magnetic).
Cr – Corrosion Resistance.
Mo – High temperature Strength, Resist Hydrogen embrittlement (Traps Hydrogen atoms and prevents their diffusivity).
Mn – Improves hot working properties, helps in removing impurities in steel production.
Si – Acts as deoxidiser in steel production
S and P – Improves machinability when added in small amounts. (Detrimental effects on corrosion resistance and weldability)
N – Pitting corrosion resistance.
Sensitization – Material becomes susceptible to intergranular corrosion due to the formation of chromium carbides.

## Slide 4
316L Steel
Characteristics:
High Creep Resistance
Excellent Formability
Corrosion Resistance
High Temperature Tensile strength
Applications:
Chemical Industry
Petroleum Refining Equipment
Heat Exchanger Tubes
Evaporators
Marine Applications
Automotive and Aerospace
https://www.lenntech.com/stainless-steel-316l.htm

## Slide 5
Additive Manufacturing
Additive manufacturing, also known as 3D printing, is a process used to fabricate a physical object from a 3D digital model, typically by laying down and bonding many successive thin layers of materials.
8 Steps of any
Additive Manufacturing Process
Advantages:
Rapid Process.
Design Freedom and Customization.
Cleaner, Streamlined, and Versatile Workshops.
Disadvantages:
High initial costs.
Size constraints.
Material Limitations.
Ian, David, Brent, Additive Manufacturing Technologies.

## Slide 6
Additive Manufacturing
Types of Additive Manufacturing Processes:

## Slide 7
Directed Energy Deposition
Directed Energy Deposition (DED) processes direct energy into a narrow, focused region to heat a substrate, melting the substrate and simultaneously melting material that is being deposited into the substrate’s melt pool.
melt materials as they are being deposited
Laser based Powder DED
Advantages
A broad range of feedstock materials.
Manufacturing of larger parts is possible compared to PBF.
High deposition rates.
Ian, David, Brent, Additive Manufacturing Technologies.
Notes: The energy density of the beam must be above a critical value to form a melt pool.

## Slide 8
Bragg’s Law
Diffraction of x-rays by a crystal.
Path Difference betweenand
This implies that andare in same phase.
B.D. Cullity, S.R. Stock, Elements of X-Ray Diffraction

## Slide 9
Rays 1 and 2 are scattered by atoms K and L, and the path difference for rays and is given by :
Bragg’s Law
B.D. Cullity, S.R. Stock, Elements of X-Ray Diffraction
Diffraction of x-rays by a crystal.
For Constructive Interference:
(where n = 1,2,3…)
Notes: Phase difference = (2pi/wavelength)*path difference

## Slide 10
XRD
XRD is a high-precision non-destructive technique that provides important information about the structural characteristics of the materials by enabling chemical composition identification.
Every crystalline substance gives a pattern; the same substance always gives the same pattern; and in a mixture of substances, each produces its pattern independently of the others – Hull (1919).
Working Principle of XRD:
X-rays from the tube T are incident on a crystal C which may be set at any desired angle to the incident beam by rotation about an axis through O. D is a detector which measures the intensity of the diffracted x-rays.
Schematic of XRD
B.D. Cullity, S.R. Stock, Elements of X-Ray Diffraction
Notes: Why angle with plane is considered and not angle with normal?

## Slide 11
XRD
Structure Factor: The resultant wave scattered by all the atoms of the unit cell.
where, is the Structure Factor for atomic plane.
is the Atomic Scattering Factor of atom.
are the co-ordinates of the position of atom.
B.D. Cullity, S.R. Stock, Elements of X-Ray Diffraction

## Slide 12
XRD
Structure Factor for FCC Unit cell: The FCC unit cell contains 4 atoms. These 4 atoms are positioned at the following fractional coordinates within the unit cell -
(for unmixed indices) (for mixed indices)
Thus, reflections may occur for such planes as (111),(200),and (220) etc

## Slide 13
XRD
Peak Broadening: XRD peaks broaden due to 3 factors –
Size broadening
Strain broadening
Instrument broadening
Size Broadening:
Where, - Crystallite Size.
- Incident radiation wavelength.
- peak broadening due to size
- Half of diffraction angle.
- Shape Factor ( = 0.9 for spherical particles)
Scherrer’s Equation

## Slide 14
XRD
Size Broadening: Differentiating Bragg’s law yields the relation between the strain and strain broadening.
In this case, strain is defined as
For a change in the interplanar spacing (), there is a corresponding change in the Bragg angle ()
Assuming is small, and

## Slide 15
XRD
( negative sign indicates direction of peak shift)

## Slide 16
XRD
Instrument Broadening: This refers to the additional broadening of diffraction peaks caused by imperfections and limitations of the instrument itself, rather than the sample.
Detector resolution
Crystal imperfections in optics
Instrument vibrations
X-ray source size
Factors contributing to Instrument Broadening:
Notes: Limited resolution of the detector used to measure the diffraction pattern can contribute to peak broadening.
Imperfections in monochromators or focusing crystals within the X-ray instrument can distort the beam and broaden peaks.
Mechanical vibrations within the instrument can also cause broadening.
The finite size of the X-ray source can lead to divergence, which affects the resolution and broadens the peaks.

## Slide 17
Curve Fitting
Curve fitting of a X-ray diffractogram is essential because:
Accurate Peak identification
Quantitative Analysis
Noise Reduction
The Gaussian function is often the best choice for fitting a X-ray diffractogram due to its ability to accurately represent the shape of diffraction peaks, which are typically symmetrical and bell-shaped.
Gauss Function –
Where, – Peak Height (Amplitude).
– Standard deviation.
– Peak Position.
FWHM occurs at
Notes: Curve fitting is a process of finding a mathematical function that best represents a set of data points.

## Slide 18
Strain Calculation
Since Gaussian broadening combines quadratically, the relation becomes additive in terms of squares.
Where
c =
Therefore, Strain and Crystallite size can be estimated from this relation.
B.D. Cullity, S.R. Stock, Elements of X-Ray Diffraction

## Slide 19
Dislocation Density
G. K. Williamson & R. E. Smallman (1956)
Dislocation Density () is be defined as:
This Equation can be written as:
Where, is the strain
b is the burgers vector
For FCC metals, K = 16.1 and along [110] direction

## Slide 20
Experimental Procedure
Sample Preparation: 1300W_DED_316L steel samples were cut using an Electric Discharge Machine (EDM).
TGA: To assess the thermal stability and potential weight loss of the samples at elevated temperatures, TGA was conducted.
XRD: XRD measurements were performed on the samples to analyse their crystallographic structure. The samples were heated to 400°C, 600°C, 800°C, 1000°C, and 1150°C, and after reaching each temperature, XRD readings were recorded. An initial reading was taken at 25°C for all samples before heating.
Inverted Microscope and Vickers Hardness Tester were used to obtain microstructures and hardness values respectively.

## Slide 21
XRD Parameters
High Temperature XRD of 1300W DED 316L sample is performed at 400°C, 600°C, 800°C, 1000°C, and 1150°C.
Incident radiation wavelength - = 1.5406 Å
Scan Mode – Continuous
Scan Rate – 300 scans per minute
Sensitivity in measurement –
X-ray Tube parameters –
Cathode – Tungsten; Anode – Copper; Voltage – 45kV; Current – 30mA
Sample Stage – Pt heat strip (direct heating)
Thermocouple – Pt 10% RhPt

## Slide 22
Results
TGA
The initial dip is attributed to the removal of porosity within the material, followed by a stable ascend.
The absence of significant weight loss throughout the analysis confirmed that no mass loss occurred, indicating the sample's readiness for subsequent high-temperature XRD measurements.

## Slide 23
Results
Determining Crystal Structure
Peak No. | d-Spacing (Å) | 1/d2 | Ratio | Ratio * 2 | Ratio * 3
1 | 2.06 | 0.24 | 1.00 (Peak 1 / Peak 1) | 2.00 | 3.00
2 | 1.79 | 0.31 | 1.32 (Peak 2 / Peak 1) | 2.64 | 3.98
3 | 1.27 | 0.64 | 2.67 (Peak 3 / Peak 1) | 5.34 | 8.01
The ratio of final values is 3 : 3.98 : 8.01.
The ratio of first 3 peaks of FCC is 3 : 4 : 8.
Therefore, Crystal structure of 316L steel is FCC.
(Degrees)

## Slide 24
Results
XRD at 400°C
Heating Cycle
25°C
400°C
20°C/min
-20°C/min

## Slide 25
Results
XRD at 400°C
Peak Position (2θ) | FWHM (β)
43.97° | 0.30°
51.00° | 0.56°
74.93° | 0.48°
At 25°C
At 400°C
Peak Position (2θ) | FWHM (β)
43.85° | 0.30°
50.87° | 0.54°
74.70° | 0.45°
(Degrees)

## Slide 26
Results
XRD at 600°C
Heating Cycle
25°C
600°C
20°C/min
-20°C/min

## Slide 27
Results
XRD at 600°C
Peak Position (2θ) | FWHM (β)
44.00° | 0.27°
51.00° | 0.58°
74.96° | 0.42°
At 25°C
At 600°C
Peak Position (2θ) | FWHM (β)
43.71° | 0.27°
50.68° | 0.58°
74.43° | 0.41°
(Degrees)

## Slide 28
Results
XRD at 800°C
Heating Cycle
25°C
800°C
20°C/min
-20°C/min

## Slide 29
Results
XRD at 800°C
Peak Position (2θ) | FWHM (β)
44.03° | 0.27°
51.08° | 0.45°
75.00° | 0.48°
At 25°C
At 800°C
Peak Position (2θ) | FWHM (β)
43.67° | 0.25°
50.66° | 0.46°
74.30° | 0.46°
(Degrees)

## Slide 30
Results
XRD at 1000°C
Heating Cycle
25°C
1000°C
20°C/min
-20°C/min

## Slide 31
Results
XRD at 1000°C
Peak Position (2θ) | FWHM (β)
44.07° | 0.24°
51.16° | 0.31°
75.02° | 0.54°
At 25°C
At 1000°C
Peak Position (2θ) | FWHM (β)
43.52° | 0.21°
50.51° | 0.28°
73.97° | 0.45°
(Degrees)

## Slide 32
Results
XRD at 1150°C
Heating Cycle
25°C
1150°C
20°C/min
-20°C/min

## Slide 33
Results
XRD at 1150°C
Peak Position (2θ) | FWHM (β)
44.07° | 0.32°
51.14° | 0.48°
75.02° | 0.54°
At 25°C
At 1150°C
Peak Position (2θ) | FWHM (β)
43.56° | 0.22°
50.57° | 0.33°
73.96° | 0.43°
(Degrees)

## Slide 34
Results
Dislocation Density at 400°C
25°C
400°C
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
400°C |  |  | 
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
400°C |  |  | 

## Slide 35
Results
Dislocation Density at 600°C
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
600°C |  |  | 
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
600°C |  |  | 
25°C
600°C

## Slide 36
Results
Dislocation Density at 800°C
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
800°C |  |  | 
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
800°C |  |  | 
25°C
800°C

## Slide 37
Results
Dislocation Density at 1000°C
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
1000°C |  |  | 
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
1000°C |  |  | 
25°C
1000°C

## Slide 38
Results
Dislocation Density at 1150°C
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
1150°C |  |  | 
 | Crystallite Size (nm) | Strain | Dislocation Density (m-2)
25°C |  |  | 
1150°C |  |  | 
25°C
1150°C

## Slide 39
Results
Microstructures
400°C
5.93 μm
600°C
6.93 μm
800°C
7.48 μm
1000°C
12.45 μm
1150°C
8.82 μm

## Slide 40
Analysis
Peak Shift vs Temperature
Chart: Temperature
| 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 0.12 | 0.29 | 0.36 | 0.55 | 0.51
(111) Peak

## Slide 41
Analysis
Peak Shift vs Temperature
(200) Peak
Chart: Temperature
| 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 0.13 | 0.32 | 0.42 | 0.65 | 0.57

## Slide 42
Analysis
Peak Shift vs Temperature
(220) Peak
Chart: Temperature
| 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 0.23 | 0.53 | 0.7 | 1.05 | 1.06

## Slide 43
Analysis
Reason for peak shift at elevated temperatures
Representation of an actual lattice showing misorientation
A crystal does not have its atoms arranged on a perfectly regular lattice extending from one side of the crystal to the other.
Let’s say “𝛼” is the maximum misorientation angle.
If “𝜃” is the incident beam angle, diffraction occurs around “𝜃+ 𝛼.”
“𝛼” decreases at elevated temperatures due to “polygonization” thus causing peak shift towards left side.

## Slide 44
Analysis
Lattice Parameter vs Temperature
Lattice Parameter
Chart: Temperature
| 25°C | 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 3.56 | 3.58 | 3.6 | 3.61 | 3.62 | 3.63

## Slide 45
Analysis
Grain Size vs Temperature
Chart: Temperature
| 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 5.93 | 6.93 | 7.48 | 12.45 | 8.82

## Slide 46
Analysis
Strain vs Temperature
Chart: Temperature
| 25°C | 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 6.2 | 5.43 | 5.4 | 5.38 | 5.36 | 5.32

## Slide 47
Analysis
Dislocation Density vs Temperature
Chart: Temperature
| 25°C | 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 9.76 | 7.42 | 7.26 | 7.15 | 7.07 | 6.91

## Slide 48
Analysis
Hardness vs Temperature
Chart: Temperature
| 400°C | 600°C | 800°C | 1000°C | 1150°C
 | 207.33 | 202.49 | 194.25 | 192.05 | 187.6

## Slide 49
Thank You!

## Slide 50
400°C
600°C